## Slide 1
Specimen | c in MPa | d in MPa
HL | 0.044 | 0.014
HM | 0.051 | 0.016
HS | 0.067 | 0.018
RL | 0.031 | 0.011
RM | 0.065 | 0.018
RS | 0.093 | 0.02
Additional File 5
Notes: Additional File 5: Neo-Hookean material parameters for different particle types and sizes as estimated using least squares fit to compression test data.