Appendix

Richart et al. 66 proposed the following form to relate the compressive strength of confined concrete fcc and the peak strain ϵcc to the lateral confining pressure fl.

| fcc=fco1+k1flfco | (A1) |
| --- | --- |
| ϵcc=ϵco1+k2flfco | (A2) |

where k1 and k2 are coefficients estimated by the regression on experimental data, fco is the compressive strength in an unstrengthened condition, and ϵco is the compressive strain corresponding to fco.  According to Pellegrino and Modena 50, the total confining pressure fu is computed as the sum of flf and fls reduced by the ratio Acc/Ag, where Acc is the area of concrete core measured from outside the transverse reinforcement and Ag is the gross area of the section.

| fu=flf+flsAccAg | (A3) |
| --- | --- |

It is established that the efficiency of exterior wraps is better on circular sections as compared to rectilinear sections 48,50,60,67. This is because the cross-section of a circular section is fully confined. On the contrary, the presence of sharp corners induces stress concentrations that result in the reduced efficiency of external wraps 35. The lateral confining pressure by the FRRP sheet is related to the external confinement by Eq. (A4).

| flf=2fttfnfD×kef | (A4) |
| --- | --- |

where ft is the rupture capacity of FRRP, tf is the thickness of FRRP, nf is the number of FRRP layers applied, D is the size of the section, and kef is a factor that accounts for the reduced efficiency of FRRP wraps due to corners. For a circular section, D is its diameter, whereas the D is replaced by an equivalent value defined by Eq. (A5) and shown in Figure A1 35.

| D=2bdb+d | (A5) |
| --- | --- |

where b is the width and d is the depth of the section.

Figure A1. Description of bursting pressure and forces in FRRP sheet

The coefficient kef is defined as the product of kvf and khf, where kvf is a factor that considers the reduced efficiency of FRRP wraps along the height of the specimen. For continuous FRRP wraps as used in this study, the term kvf is taken as 1.0. The factor khf considers the reduced efficiency of FRRP wraps within a section. For a circular section, the factor khf is taken as 1.0, whereas khf is calculated using Eq. (A6) 60,65.

| khf=1-wx2+wy23bd1-ρcc | (A6) |
| --- | --- |

where wx and wy are defined in Figure 16a and ρcc is the volumetric ratio of the longitudinal reinforcement. The definition of the confinement pressure due to internal transverse reinforcement is adopted from Mander et al. 65, defined in Eq. (A7) and illustrated in Figure A2.

| fls=12kesρstfyt | (A7) |
| --- | --- |

where ρst and fyt are the volumetric ratio and yield strength of transverse reinforcement, respectively. The coefficient kes defines the reduction in the efficiency of transverse reinforcement due to sharp corners in rectilinear sections and the discontinuity of transverse reinforcement along the height of the specimen and defined as:

| kes=kvs×khs | (A8) |
| --- | --- |

where khs is a factor that considers the ineffectively confined areas within a section. For circular sections, khs is taken as 1.0, whereas khs is defined in Eq. (A9) and shown in Figure 16b for rectilinear sections 50,60,65. Similarly, the parameter kvs incorporates the ineffectively confined areas along the height of the specimen, as defined in Eq. (A10).

| khs=1-wxi2+wyi26xy1-ρcc | (A9) |
| --- | --- |
| kvs=1-s'2x1-s'2y1-ρcc | (A10) |

where ρcc is the longitudinal reinforcement volumetric ratio, s' is the clear distance between consecutive hoops, and x and y are defined in Figure A2b.

Figure A2. Definition of confined areas along a rectangular section (a) by FRP and (b) by internal steel reinforcement.