SUPPLEMENTARY

Optimizing the Thermal and Mechanical Performance of PLA Reinforced with Surface-Treated HEMP Biocomposite for Automotive Applications

Sifiso John Skosana1. Caroline Khoathane1. Thomas Malwela2. Wilson Webo1

1Department of Chemical, Metallurgical and Materials Engineering, Faculty of Engineering and the Built Environment, Tshwane University of Technology, Pretoria 0001, South Africa

2Departmet of Physics, University of Limpopo, Private Bag X1106, Sovenga 0727, South Africa

Corresponding Author. Emails: thomas.malwela@ul.ac.za

Table S1: Parameters and characteristics of the Factors for the printing process

| Factor | Name | Units | Type | SubType | Minimum | Maximum | Coded Low | Coded High | Mean | Std. Dev. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| A | Volume Fraction | % | Numeric | Continuous | 1.00 | 20.00 | -1 ↔ 1.00 | +1 ↔ 20.00 | 11.01 | 7.47 |
| B | Print Velocity | mm/s | Numeric | Continuous | 40.00 | 60.00 | -1 ↔ 40.00 | +1 ↔ 60.00 | 49.55 | 7.55 |
| C | Nozzle Diameter | mm | Categoric | Nominal | 0.4 | 2 |  |  | Levels: | 3.00 |
| D | Printing Direction | ° | Categoric | Nominal | 0 | 90 |  |  | Levels: | 3.00 |

Table S2: Parameters and characteristics of the Reponses for the printing process

| Response | Name | Units | Observations | Minimum | Maximum | Mean | Std. Dev. | Ratio |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| R1 | Elastic Modulus | MPa | 32.00 | 1485.5 | 3275.3 | 2192.85 | 371.54 | 2.20 |
| R2 | Impact Strength | MPa | 32.00 | 5.12 | 25.14 | 11.95 | 5.57 | 4.91 |
| R3 | Thermal Degradation Temperature | ° C | 32.00 | 292.17 | 352.5 | 317.83 | 16.47 | 1.21 |

| Table S3: Constraints characteristics of the Factors and Responses for the printing process |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Name | Goal | Lower Limit | Upper Limit | Lower Weight | Upper Weight | Importance |
| A:Volume Fraction | is in range | 1 | 20 | 1 | 1 | 3 |
| B:Print Velocity | is in range | 40 | 60 | 1 | 1 | 3 |
| C:Nozzle Diameter | is in range | 0.4 | 2 | 1 | 1 | 3 |
| D:Printing Direction | is in range | 0 | 90 | 1 | 1 | 3 |
| Elastic Modulus | maximize | 1485.5 | 3275.3 | 1 | 1 | 3 |
| Impact Strength | maximize | 5.12 | 25.14 | 1 | 1 | 3 |
| Thermal Degradation Temperature | maximize | 292.17 | 352.5 | 1 | 1 | 3 |

Table S4: 5 of the 63 Solutions found for the desirability analysis.

| Table S4: 5 of the 63 Solutions found for the desirability analysis. |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Number | Volume Fraction | Print Velocity | Nozzle Diameter | Printing Direction | Elastic Modulus | Impact Strength | Thermal Degradation Temperature | Desirability |  |
| 1 | 1.000 | 40.000 | 1 | 45 | 3005.242 | 19.748 | 337.675 | 0.776 | Selected |
| 2 | 1.289 | 40.000 | 1 | 45 | 3008.195 | 19.749 | 336.797 | 0.772 |  |
| 3 | 1.000 | 40.000 | 2 | 45 | 2760.173 | 21.582 | 338.644 | 0.767 |  |
| 4 | 1.000 | 40.081 | 2 | 45 | 2755.637 | 21.565 | 338.642 | 0.766 |  |
| 5 | 1.143 | 40.000 | 2 | 45 | 2761.642 | 21.583 | 338.122 | 0.764 |  |

Figure S1: Response surface and contour plots illustrating the effects of volume fraction (A) and print velocity (B) on the elastic modulus of PLA reinforced with surface-treated hemp biocomposites under various processing conditions. Subplots (a-i) represent different combinations of nozzle diameter and printing direction: (a,d,g) 0.4 mm nozzle; (b,e,h) 1.0 mm nozzle; (c,f,i) 2.0 mm nozzle; (a,b,c) 0° printing direction; (d,e,f) 45° printing direction; (g,h,i) 90° printing direction. The color gradients and contour lines indicate the magnitude of the elastic modulus, with warmer colors representing higher values.

Figure S2: 3D contour plots illustrating the effects of volume fraction (A) and print velocity (B) on the impact strength of PLA reinforced with surface-treated hemp biocomposites under various processing conditions. Subplots (a-i) represent different combinations of nozzle diameter and printing direction: (a,d,g) 0.4 mm nozzle; (b,e,h) 1.0 mm nozzle; (c,f,i) 2.0 mm nozzle; (a,b,c) 0° printing direction; (d,e,f) 45° printing direction; (g,h,i) 90° printing direction. The color gradients and contour lines indicate the magnitude of the elastic modulus, with warmer colors representing higher values.

Figure S3: 3D contour plots illustrating the effects of volume fraction (A) and print velocity (B) on the thermal stability of PLA reinforced with surface-treated hemp biocomposites under various processing conditions. Subplots (a-i) represent different combinations of nozzle diameter and printing direction: (a,d,g) 0.4 mm nozzle; (b,e,h) 1.0 mm nozzle; (c,f,i) 2.0 mm nozzle; (a,b,c) 0° printing direction; (d,e,f) 45° printing direction; (g,h,i) 90° printing direction. The color gradients and contour lines indicate the magnitude of the elastic modulus, with warmer colors representing higher values.

Figure S4: Desirability analysis for optimizing PLA/surface-treated hemp fiber composites. The graph shows the desirability scores for input factors (volume fraction, print velocity, nozzle diameter, and printing direction) and output responses (elastic modulus, impact strength, and thermal degradation temperature). The combined desirability score represents the overall optimization outcome for the composite material intended for automotive applications. Input factors show maximum desirability (1.0), while output responses and the combined score indicate the degree of optimization achieved for each property.